|  |  |  |
| --- | --- | --- |
| **Modules** | **Description** | **Enabled devices** |
| 2 SiN flavors | 2 SiN thicknesses: 150nm (BioPIX150) 300nm (BioPIX300) | 2 flavors optimized for wavelengths 300nm – 1000nm |
| 2 SiN patterning steps each | 2 etch depths BioPIX150: 90nm / 150nm BioPIX300: 150nm / 300nm | Strip / rib waveguides, shallow etched grating couplers |
| Clad oxide removal | Exposure of waveguides for sensing by removing local clad SiO2 | Micro-channels for evanescent sensing by waveguides. |
| Metal heater | TiN metal lines for resistive heating | Thermo-optic tuners, switches, modulators etc. |
| Metal interconnect | Al metal lines and pads for interconnects | Metal interconnects, probe-pads, bond-pads |
| Deep trench | Deep trench to expose edge coupler facets | Edge couplers |

PIX4life

BioPIX platform